TECHNICAL DATA SHEET

HS CLEARCOAT CERAMIC

Product code: 80949

PRODUCT DESCRIPTION

Clearcoat in Premium segment is characterized by high content of solids. High hardness, resistance to weather conditions, UV rays and stone impact. Coating does not chip off even with strong strokes of stones. Has excellent gloss and excellent flow. It is characterized by high elasticity and hardness which guarantees "colour depth" effect.

| MIXING RATIO |  |  |
| --- | --- | --- |
|  | A: Clearcoat HS CERAMIC | 100 |
|  | B: Hardener HS CERAMIC | 50 |
| Comments: | Due to the habits of painters, mixture of clearcoat and hardener can be diluted with C: acryl thinner in the ratio 5-10% of weight of the clearcoat. |  |
|  | When spraying without thinner, texture will has orange peel look. |  |
| APPLICATION |  |  |
|  | Number of layers | 2 or 1,5 |
|  | Pressure | 2 - 2,5 bar |
|  | Nozzle | 1.3 - 1.4 mm |
|  | Flash off between layers | 10 - 12 min |
|  | Mixture life after mixing clearcoat with standard type of hardener | 60 min at 20°C |

The first half-layer of clearcoat (1,5 layer system) or first full layer of clearcoat (2 layers system) is applied to the pre-dried layer of basecoat. Second layer of clearcoat should be applied as a full layer and left to complete flow and hardening. Coating of clearcoat can be hardened by using IR heater. Please note that IR heater should not be turned on earlier than after about 15 minutes after application last layer of clearcoat. When painting large surfaces it is recommended to use a hardener and the acryl thinner - slow version.

| ADDITIONAL INFORMATION |  |  |
| --- | --- | --- |
|  | Viscosity (DIN 4/20°C) |  |
|  | Without thinner | 18 - 19 s |
|  | After adding thinner | 16 - 17 s |
|  | Operating hardness | 14 h at 20°C |
|  |  | 45 min at 50°C |
|  | Ending hardness | 4 days |
|  | Dust-free | 35 min at 20°C |
|  |  | 5 min at 50°C |

Hardness tested after 14 days in accordance with EN ISO 1522 Persoz pendulum – 352

| CONTENT OF VOLATILE ORGANIC COMPOUNDS |  |
| --- | --- |
| Maximum content of VOC in product | 460 g/l |
| VOC for category: II,B/e | 840 g/l |

Clearcoat complies standards of EU Directive 2004/42/CE/II,B/e(840)

STORAGE TIME AND CONDITIONS

CLEANING EQUIPMENT

Store in tightly closed containers, in a cool, dry place away from sources of fire and heat. Avoid exposure to sunlight.

Expiration date: 12 months from date of manufacture - date on the top of container.

For cleaning equipment can be used acryl thinner or nitro thinner. It is recommended to use thinner for cleaning paint spray guns.

HEALTH AND SAFETY REGULATIONS

SPECIFIC WEIGHT

See Safety Data Sheet of the product.

About 1.0 g/cm3

OTHER INFORMATION

The effectiveness of our systems results from laboratory research and many years of experience. The data contained herein meets the current knowledge about our products and their application potential. We ensure high quality, provided the user follows the instructions and the work is performed in accordance with good workmanship. It is necessary to do a test application of the product due to its potentially different reaction with different materials. We may not be held liable for defects if the final result was affected by factors beyond our control. RAGS Ltd., Reg. No.: 40003133752, VAT number: LV40003133752 Legal address: Durbes street 8, Rīga, LV-1007, Actual address: Džūkstes street 1, Rīga, LV-1004 Tel. +371 67 808 780, +371 26 542 777