TECHNICAL DATA SHEET

VHS EXPRESS CLEARCOAT

Product code: 80926

PRODUCT DESCRIPTION

VHS clearcoat with increased scratch resistance and extremely short curing times. Clearcoat can  be polished already after 3 hours at 20°C or after 5 minutes at 60°C. Long open time allows to paint large areas and entire cars. The coating has a high gloss, high hardness and scratch resistance.

| MIXING RATIO |  |  |
| --- | --- | --- |
|  | A: Clearcoat VHS Express | 100 |
|  | B: Hardener VHS Express | 50 |
| Comments: | Use without thinner. |  |
| APPLICATION |  |  |
|  | Number of layers | 1,5 |
|  | Pressure | 2 - 2,5 bar |
|  | Nozzle | 1.2 - 1.4 mm |
|  | Flash off between layers | 8-10 min |
|  | Mixture life after mixing clearcoat with hardener | 40 min at 20°C |

The first half-layer of clearcoat should be applied on the pre-dried layer of basecoat.

Second layer of clearcoat should be applied as a full layer and left to complete flow and hardening.

In case of using spraying booth, after second layer painter should wait 10 minutes and after that time turn on spray booth on 50°C heating level.

| ADDITIONAL INFORMATION |  |  |
| --- | --- | --- |
|  | Viscosity (DIN 4/20°C) | 17 – 19 s |
|  | Dust dry | 20 min at 20°C |
|  | Tack-free | 2 h at 20°C |
|  | Operating hardness (polishability) | 3 h at 20°C |
|  |  | 5 min at 60°C |
|  | Ending hardness | 3 days |
| CONTENT OF VOLATILE ORGANIC COMPOUNDS |  |  |
| Maximum content of VOC in product |  | 480 g/l |
| VOC for category: II,B/e |  | 840 g/l |

Clearcoat complies standards of EU Directive 2004/42/CE/II,B/e (840)

STORAGE TIME AND CONDITIONS

CLEANING EQUIPMENT

Store in tightly closed containers, in a cool, dry place away from sources of fire and heat. Avoid exposure to sunlight. Expiration date: 12 months from date of manufacture - date on the top of container.

For cleaning equipment can be used acryl thinner or nitro thinner. It is recommended to use thinner for cleaning paint spray guns.

HEALTH AND SAFETY REGULATIONS

SPECIFIC WEIGHT

See Safety Data Sheet of the product.

About 1.0 g/cm3

OTHER INFORMATION

The effectiveness of our systems results from laboratory research and many years of experience. The data contained herein meets the current knowledge about our products and their application potential. We ensure high quality, provided the user follows the instructions and the work is performed in accordance with good workmanship. It is necessary to do a test application of the product due to its potentially different reaction with different materials. We may not be held liable for defects if the final result was affected by factors beyond our control. RAGS Ltd., Reg. No.: 40003133752, VAT number: LV40003133752 Legal address: Durbes street 8, Rīga, LV-1007, Actual address: Džūkstes street 1, Rīga, LV-1004 Tel. +371 67 808 780, +371 26 542 777