# TECHNICAL INFORMATION

FOR PROFESSIONAL USE ONLY

| CRYSTAL CLEAR COAT VHS 2:1 ACRYLIC CLEAR COAT ULTIMATE RAPID DRYING VHS 2:1 |  |  |  |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- | --- |
| PRODUCTS |  |  |  |  |  |  |  |  |
| CRYSTAL Clear Coat VHS 2:1 Hardener STANDARD 1:2 for CRYSTAL Clear Coat VHS Hardener FAST 1:2 for CRYSTAL Clear Coat VHS |  |  |  |  |  |  |  |  |
| PRODUCT DESCRIPTION |  |  |  |  |  |  |  |  |
| High quality 2K acrylic clear coat for fast car repairs with a very low content of volatile compounds. CRYSTAL Clear Coat is designed for car paint shops that struggle every day with the problem of quickly returning the repaired vehicles to their owners. The use of the new generation of raw materials helped to achieve fast curing time.* - Very high content of resin. - Extremely high gloss. - Excellent look of the coat. * ambient temperature 20oC, humidity below 80%. |  |  |  |  |  |  |  |  |
|  |  |  |  |  |  | COLOUR: transparent |  |  |
|  |  |  |  |  |  | GLOSS GRADE: high gloss |  |  |
| VOLATILE ORGANIC COMPOUNDS |  |  |  |  |  |  |  |  |
| VOC for mixture = 355 [g/l], The share of VOC is below 540 g/l. These products meet the EU directive (2004/42/EC/II B) that sets the VOC value for its category (d), at 420 g/l. |  |  |  |  |  |  |  |  |
| SURFACE PREPARATION |  |  |  |  |  |  |  |  |
| Crystal Clear Coats can be applied over: - Base Coats, - Old finishes in good condition after matting and degreasing. |  |  | For matting we recommend the following: - grey abrasive fabric with a polishing compound, - sanding paper with gradation of 600÷800 (wet sanding), - sanding paper with gradation of 360÷500 (machine sanding). |  |  |  |  |  |
| APPLICATION PROCESS |  |  |  |  |  |  |  |  |
|  | USE |  |  |  | HARDENING TIME |  |  |  |
|  | Fast car body paint. |  |  |  |  |  |  |  |
|  |  |  |  |  | Hardening time at 20° C |  | STANDARD | FAST |
|  |  |  |  |  | Dust dry |  | 30÷35 min. | 20÷25 min. |
|  | MIXING RATIO | by volume |  |  |  |  |  |  |
|  | Clear Coat | 2 parts |  |  | Touch dry |  | 90 minutes | 60 minutes |
|  | Hardener | 1 part |  |  |  |  |  |  |
|  |  |  |  |  | Before baking |  | 10 minutes | 10 minutes |
|  | The Clear Coat does not need to be used with a thinner! |  |  |  |  |  |  |  |
|  |  |  |  |  | Baking at 60°C (temperature of baked object) |  | 5 minutes | - |
|  | SPRAYING VISCOSITY |  |  |  |  |  |  |  |
|  | 19÷21 seconds at 20oC/DIN4. |  |  |  |  |  |  |  |
|  |  |  |  |  | Temperature below 20oC significantly increases the hardening time. |  |  |  |
|  | POT LIFE |  |  |  |  |  |  |  |
|  | Hardener STANDARD: 90 minutes at 20oC Hardener FAST: 60 minutes at 20oC |  |  |  |  |  |  |  |
|  | NUMBER OF LAYERS |  |  |  | IR DRYING |  |  |  |
|  | 1.5 layers – 1 medium (thin) and then a full layer with 2 minutes of flash off between the layers in order to obtain a dry film thickness of 50-60 μm. RP gun parameters: Nozzle: 1.2÷1.4mm; Pressure of input: 2.0÷2.2bars. HVLP gun parameters: Nozzle: 1.3÷1.4mm; Inlet pressure: 2.0 bars. Note: follow the gun producer’s recommendations. |  |  |  | 5÷7 minutes of short waves, depending on the layer thickness and the type of radiator. Do not exceed 60oC. Use as recommended by the equipment manufacturer. Wait about 10 minutes before starting the heater drying. |  |  |  |

| PRODUCT EFFICIENCY |  |
| --- | --- |
| 1 liter of mixture is enough to cover 10÷11 m2 with a dry layer with thickness of 60 μm. |  |
| SHADING |  |
| Make sure that you cover the whole area with the base coat and shade only the prepared area. Use FADE OUT THINNER for shading to blend the dust that has settled around the fixing surface and compensate the optical differences in gloss between the old lacquer coat and the newly imposed acrylic clear coat. |  |
| POLISHING AND REMOVING IMPURITY INCLUSIONS |  |
| Usually polishing is unnecessary, as the VHS Clear Coat 2:1 gives the surface a perfect look immediately after application. However, if some dirt inclusions appear, we recommend removing them and then polishing the surface with an abrasive compound. |  |
| GENERAL NOTES |  |
| - Do not exceed recommended doses of hardener! - Best results achieved at room temperature. The ambient temperature and the temperature of the used product should be the same. - When working with 2K products, it is recommended to use personal protective equipment. Protect the eyes and the respiratory system. - The rooms should be well ventilated. - Clean the guns and equipment immediately after use. Caution: To maintain safety, always follow the instructions given in the MSDS for the product. |  |
| STORAGE |  |
| Store the product components between 15 and 25oC, in a sealed container, in dry and cool places, away from fire and heat sources, as well as direct sunlight. Caution: - Close the containers immediately after application. - Protect hardener against freeze and humidity! |  |
| WARRANTY PERIOD |  |
| Crystal Clear Coat VHS 2:1 Hardener STANDARD 1:2 for Crystal Clear Coat Hardener FAST 1:2 for Crystal Clear Coat | - 24 months from the date of production - 12 months from the date of production - 12 months from the date of production |

OTHER INFORMATION

The effectiveness of our systems results from laboratory research and many years of experience. The data contained herein meets the current knowledge about our products and their application potential. We ensure high quality, provided the user follows the instructions and the work is performed in accordance with good workmanship. It is necessary to do a test application of the product due to its potentially different reaction with different materials. We may not be held liable for defects if the final result was affected by factors beyond our control. RAGS Ltd. Reg. No.: 40003133752, VAT number: LV40003133752 Legal address: Durbes street 8, Rīga, LV-1007, Actual address: Džūkstes street 1, Rīga, LV-1004 Tel. +371 67 808 780, +371 26 542 777