TECHNICAL DATA SHEET

STONDER PRIMER FILLER SPRAY – One-component, filling acrylic primer intended for levelling surfaces coated with putty and old paint coatings. Perfect for spot repairs. Very short drying time allowing for making quick repairs is the main advantage of the primer.

VOC II/B/e limit = 840g/l, VOC = 656 g/l.

SHELF LIFE 48 months/20°C

| Vol. (ml) | Name | Article no. | Colour | units/pack. |
| --- | --- | --- | --- | --- |
| 500 Spray | Stonder Primer Filler Spray | 80117 | Light Grey | 12 |
|  |  | 80118 | Grey | 12 |
|  |  | 80141 | Black | 12 |
|  |  | 80142 | White | 12 |

| Shake for 2 min. | Apply 2-3 coats | 5-10 min | 15-30 min./20OC 15 min./60 OC | P360-500 | P800-1000 | Clean the valve for 5 s |  |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |

SAFETY: See Safety Data Sheet.

OTHER INFORMATION

The effectiveness of our systems results from laboratory research and many years of experience. The data contained herein meets the current knowledge about our products and their application potential. We ensure high quality, provided the user follows the instructions and the work is performed in accordance with good workmanship. It is necessary to do a test application of the product due to its potentially different reaction with different materials. We may not be held liable for defects if the final result was affected by factors beyond our control.

RAGS Ltd.,  Reg. No.: 40003133752, VAT number: LV40003133752

Legal address: Durbes street 8, Rīga, LV-1007,

Actual address: Džūkstes street 1, Rīga, LV-1004

Tel. +371 67 808 780, +371 26 542 777.