Technical Data Sheet

MS CLEARCOAT PLUS 112

Product code: 80100  0,5L, 1L

PRODUCT DESCRIPTION

Clearcoat in Medium Solid system which is characterized by good hardness and resistance to UV rays. It is resistant to troublesome weather conditions. It has very good resistance to stone  impact, coating does not chip off even with strong strokes of stones. Durability and excellent  gloss gives the coating the "colour depth" effect and guarantees its high quality. Is compatible        with all solvent basecoats including water basecoats. Occurs with hardener in standard or rapid version.

| MIXING RATIO |  |  |  |
| --- | --- | --- | --- |
|  | A: Clearcoat 112 PLUS | 100 |  |
|  | B: Hardener 112 PLUS | 50 |  |
|  | C: STONDER Acryl thinner | 5% | Full flow |
|  |  | 0% | Orange peel texture |
| Comments: | Amount of thinner calculated for weight of the clearcoat. |  |  |
|  | Do not use other thinner than STONDER acryl thinner. |  |  |
| APPLICATION |  |  |  |
|  | Number of layers | 2 |  |
|  | Pressure | 2 - 2,5 bar |  |
|  | Nozzle | 1.3 - 1.4 mm |  |
|  | Flash off between layers | 10 - 12 min |  |
|  | Mixture life after mixing clearcoat with standard type of hardener | 60 min at 20°C |  |

The first layer of clearcoat is applied to the pre-dried layer of basecoat. Second layer of clearcoat should be applied as a full layer and left to complete flow and hardening. Coating of  clearcoat can be hardened by using IR heater. Please note that IR heater should not be turned  on earlier than after about 15 minutes after application last layer of clearcoat. When painting large surfaces it is recommended to use a hardener and the acryl thinner - standart version.

| ADDITIONAL INFORMATION |  |  |
| --- | --- | --- |
|  | Viscosity (DIN 4/20°C) |  |
|  | Without thinner | 16 - 17 s |
|  | After adding thinner | 15 - 16 s |
|  | Operating hardness | 14 h at 20°C |
|  |  | 45 min at 50°C |
|  | Ending hardness | 4 days |
|  | Dust-free | 20 min at 20°C |
|  |  | 3 min at 50°C |
| CONTENT OF VOLATILE ORGANIC COMPOUNDS |  |  |
| Maximum content of VOC in product |  | 562 g/l |
| VOC for category: II,B/e |  | 840 g/l |

Clearcoat complies standards of EU Directive 2004/42/CE/II,B/e(840)

STORAGE TIME AND CONDITIONS

Store in tightly closed containers, in a cool, dry place away from sources of fire and heat. Avoid exposure to

CLEANING EQUIPMENT

sunlight. Expiration date: 12 months from date of manufacture - date on the top of container.

For cleaning equipment can be used acryl thinner or nitro thinner. It is recommended to use thinner for cleaning paint spray guns.

HEALTH AND SAFETY REGULATIONS

SPECIFIC WEIGHT

See Safety Data Sheet of the product.

About 1.0 g/cm3

OTHER INFORMATION

The effectiveness of our systems results from laboratory research and many years of experience. The data contained herein meets the current knowledge about our products and their application potential. We ensure high quality, provided the user follows the instructions and the work is performed in accordance with good workmanship. It is necessary to do a test application of the product due to its potentially different reaction with different materials. We may not be held liable for defects if the final result was affected by factors beyond our control. RAGS Ltd., Reg. No.: 40003133752, VAT number: LV40003133752 Legal address: Durbes street 8, Rīga, LV-1007, Actual address: Džūkstes street 1, Rīga, LV-1004 Tel. +371 67 808 780, +371 26 542 777