# Technical data sheet

# EASY PUTTY 2

# Light putty

Product code: 76152

| PROPERTIES |  |  |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- |
| EASY PUTTY 2 – a light multifunctional putty. The use of state-of-the-art fillers resulted in a fine product with low density. The effect is very good and easy application, excellent sand ability and low shrinkage during curing. The properties combined with good adhesion allow using the product on large and small surfaces. Due to low density, it is recommended to use a higher hardener content than in regular putties. The content is around 3%. |  |  |  |  |  |  |  |
| SUBSTRATES |  |  |  |  |  |  |  |
| polyester laminates |  |  | dry sand with P80-P120 and degrease with the silicone degreaser |  |  |  |  |
| steel |  |  | degrease, dry sand with P80 – P120, degrease again |  |  |  |  |
| galvanised steel |  |  | degrease, mat with an abrasive finishing pad and degrease again |  |  |  |  |
| aluminium |  |  | degrease, mat with an abrasive finishing pad and degrease again |  |  |  |  |
| two-component acrylic fillers |  |  | degrease, dry sand with P220 – P280, degrease again |  |  |  |  |
| old paint coatings |  |  | degrease, dry sand with P220 – P280, degrease again |  |  |  |  |
| CAUTION |  |  |  |  |  |  |  |
| Do not apply polyester putty directly on top wash primers or one-component acrylic and nitrocellulose products. The putty adheres to most types of galvanised steel used today. |  |  |  |  |  |  |  |
| MIXING RATIO |  |  |  |  |  |  |  |
| 3 100 |  |  | PUTTY HARDENER |  | Volume ratio |  | Weight ratio |
|  |  |  |  |  | 100 ml 3 ml |  | 100 g 3 g |
| APPLICATION LIFE FROM MIXING WITH THE HARDENER |  |  |  |  |  |  |  |
| 3 to 6 min at 20°C. |  |  |  |  |  |  |  |
| DRYING TIME |  |  |  |  |  |  |  |
| 20 to 30 min at 20°C. The time can be shortened by heating for 10 minutes at a maximum of 60°C. |  |  |  |  |  |  |  |
| COATABILITY |  |  |  |  |  |  |  |
| Finishing polyester putty, spray polyester filler, acrylic primers |  |  |  |  |  |  |  |
| APPLICATION CONDITIONS |  |  |  |  |  |  |  |
| The minimum application temperature is +10C |  |  |  |  |  |  |  |
| APPLICATION |  |  |  |  |  |  |  |
|  | Clean and sand the surface |  |  |  |  |  |  |
|  | Degrease the surface with silicone remover |  |  |  |  |  |  |
| 3 100 | Observe the required amount of hardener. Mix the components thoroughly until a uniform colour is obtained. Weight quantity of components: Add 100 g of EASY PUTTY 2 to 3 g of Hardener. Binding time: 3 to 6 minutes at 20C |  |  |  |  |  |  |
|  | Apply a layer of 5 mm max with a putty knife. |  |  |  |  |  |  |
|  | Wait for 20 to 30 minutes (at 20°C) |  |  |  |  |  |  |
|  | rough |  |  |  |  | finish |  |
|  | P80 – P120 |  |  |  |  | P120 – P240 |  |
| COLOUR |  |  |  |  |  |  |  |
| Beige |  |  |  |  |  |  |  |
| DENSITY |  |  |  |  |  |  |  |
| 0.83 – 0.95 g/cm3 |  |  |  |  |  |  |  |
| CONTENT OF VOLATILE ORGANIC COMPOUNDS (VOC) |  |  |  |  |  |  |  |
| VOC II/B/b limit* = 250g/l |  |  |  | 90 g/l |  |  |  |
| *For ready to use mixture. |  |  |  |  |  |  |  |
| EQUIPMENT CLEANING |  |  |  |  |  |  |  |
| Acrylic thinner or NC solvent. |  |  |  |  |  |  |  |
| STORAGE CONDITIONS |  |  |  |  |  |  |  |
| Store in a cool dry room, away from sources of fire and heat. Avoid direct exposure to sunlight. |  |  |  |  |  |  |  |
| SHELF LIFE |  |  |  |  |  |  |  |
| EASY PUTTY2 1,0 L |  | 24 months/20°C |  |  |  |  |  |
| SAFETY |  |  |  |  |  |  |  |
| See Safety Data Sheet. |  |  |  |  |  |  |  |
| NOTES |  |  |  |  |  |  |  |
| Intended for professional use only. |  |  |  |  |  |  |  |
| OTHER INFORMATION |  |  |  |  |  |  |  |
| The effectiveness of our systems results from laboratory research and many years of experience. The data contained herein meets the current knowledge about our products and their application potential. We ensure high quality, provided the user follows the instructions and the work is performed in accordance with good workmanship. It is necessary to do a test application of the product due to its potentially different reaction with different materials. We may not be held liable for defects if the final result was affected by factors beyond our control. RAGS Ltd., Reg. No.: 40003133752, VAT number: LV40003133752 Legal address: Durbes street 8, Rīga, LV-1007, Actual address: Džūkstes street 1, Rīga, LV-1004 Tel. +371 67 808 780, +371 26 542 777 |  |  |  |  |  |  |  |